## Slide 1
PAKISTAN STATE OIL COMPANY LIMITED
Every journey begins here

## Slide 2
PAKISTAN STATE OIL
1
More than 55%
Market Share in POL
59%
OMC Import
1.232 MMT
47% of OMC Storage
19 Depots
9 Installations
14 Airports
3 Seaports
3500+
Retail Outlets
State of Art LMT
Capacity 50,000 MT
Lube Raw Material
Strg. Capacity 6,000 MT
Automated Filling
Keamari, Machike, Sihala
Over 3 Million
Consumers Per day
24
ISO Certified MQTUs
4,000+ OGRA Compliant
Fleet of Tank Lorries
11,000+
Fleet of Tank Lorries
Shareholding in WOPP
Karachi to MehmoodKot
We are the biggest energy company of Pakistan that has invested in the storage and retail network infrastructure alongside human capital to ensure a superior experience and best quality products to our valued consumer.
Over PKR 2.5 Trillion
Annual Turnover
First OMC to Launch
EURO-V Standard Fuels
World Class
Quality Lubricants
R&D
Customized Lubricants
Pioneer
Fuel Cards Business
Pioneer of introducing FS CK-4 HDDEO

## Slide 3
2
First to Introduce
Euro-V Standard Fuel
Automated Filling Operations at Terminal
OGRA & NHA Compliant Fleet
Tank Lorry Tracking Facility Available
ISO Certified POL Testing Laboratory
PAKISTAN STATE OIL
On-Site Fuel Testing Facility

## Slide 4
3
Diesel Gen. sets
Gear & Transmission
Hydraulic Systems
Industrial Gears
Machines & Spindles
Steam & Gas Turbines
Air Compressors
Marine Engines
Gas Engines
Thermal oil Boiler
Refrigeration Systems
Open Gears
Transformers
Metal Working
Bearing Applications
PAKISTAN STATE OIL

## Slide 5
4
PAKISTAN STATE OIL

## Slide 6
6
Bitumen based Sugar Mill Oil
Industrial Gear Oil
Greases
Hydraulic Oil
Turbine Oil
PSO Lubricants for Sugar Industry
Compressor Oil

## Slide 7
5
Continuous improvement in PSO lubricants.
Addition of new and latest lubricants to meet future requirement.
Customized solution for :
Industrial Lubricants
Automotive Lubricants
PSO LUBRICANTS-Research & Development

## Slide 8
7
PSO SYNTHETIC SMO GOLD
Available in three viscosity grades

## Slide 9
8
COMPONENTS:
Superior Synthetic Components – Balanced combination of Highly reactive and Stabilized components
High viscosity base oil
Extreme pressure additives
PSO SYNTHETIC SMO GOLD

## Slide 10
9
APPLICATIONS:
A premium lubricant specifically formulated to meet the demanding requirements of sugar mill roll bearings and gear lubrication.
Their high viscosities in combination with enhanced additive packages including tackifiers enable them to provide exceptional protection to heavily loaded slow speed roll bearings, gearboxes and open gears in applications where high volumes of process water, corrosive cane juice, dust and bagasse contamination are major challenges.
Offers the same key benefits as SUGAR MILL OIL but with the additional feature of being clear to enable visual inspection of components without the need to clean up first.
PSO SYNTHETIC SMO GOLD

## Slide 11
10
PSO SYNTHETIC SMO GOLD-Functional Benefits
Equally suitable at high operating conditions
Proper lubrication at low temperature
Smooth Oil Flowability at low temperatures
Maintains viscosity at elevated temperatures
Reduces maintenance cost and increases bearing and gear service life
Possesses high shear stability

## Slide 12
11
PSO SYNTHETIC SMO GOLD-Functional Benefits
Maintains oil film strength to keep surfaces apart
Excellent load carrying and extreme pressure handling properties
Protection against bearing wear and tear
Maintains bearing temperature even under extreme operating conditions

## Slide 13
12
PSO SYNTHETIC SMO GOLD-Functional Benefits
Supports reduced oil consumption
Improved corrosion resistance
Excellent water resistance provides
Incorporates tackiness additive

## Slide 14
PROPERTIES | METHOD | TYPICAL RESULTS |  | 
 |  | 16K | 20K | 25K
Appearance | Visual | Bright & Clear | Bright & Clear | Bright & Clear
Color | ASTM D-1500 | L 3.0 | L 3.0 | L 3.0
Density @ 15 °C, Kg/liter | ASTM D-4052 | 0.9119 | 0.9110 | 0.9101
Kinematic Viscosity @ 40 °C, cSt | ASTM D-445 | 16,100 | 20,100 | 25,100
Kinematic Viscosity @ 100 °C, cSt | ASTM D-445 | 526 | 616 | 750
Flash Point (COC), °C | ASTM D-92 | 224 | 222 | 222
Pour Point, °C | ASTM D-97 | 6 | 9 | 9
Viscosity Index | ASTM D-2270 | 176 | 180 | 190
PSO SYNTHETIC SMO GOLD-Typical Characteristics
13

## Slide 15
14
PSO SYNTHETIC SMO GOLD-Proof of Performance

## Slide 16
PSO AUTOMOTIVE LUBRICANTS
PAKISTAN STATE OIL
15

## Slide 17
PSO CARIENT Series - Petrol Engine Oil
PAKISTAN STATE OIL
16

## Slide 18
PSO DEO Series-Diesel Engine Oil
PAKISTAN STATE OIL
17

## Slide 19
API License & OEM Approval-Volvo Group Trucks Technology
PAKISTAN STATE OIL
18

## Slide 20
Used Oil Analysis Program
PSO Oil Watch Program provides lubricants after sale technical advisory services through Used Oil testing.
Used oil analysis is an important part of engine/equipment maintenance.
The program includes information sharing with customer about the condition of oil in use and its suitability for further use. Another advantage of the program is monitoring condition of engine/equipment lubricated by the oil.
PAKISTAN STATE OIL-Lubricant after sales services
19

## Slide 21
Used Oil Analysis-PSO Oil Watch Program
The program consists of detailed testing of used oil at well-equipped PSO laboratory and technical interpretation of test results and advises further to get maximum benefits of oil and optimizing oil drain intervals.
Oil testing & interpretation of results is based on sample being taken according to reliable procedure.
20
PAKISTAN STATE OIL-Lubricant after sales services
THANK YOU